- Retro-reflective markings：

  - Retro-reflective markings: means reflection-identifying material on vehicle, used to enhance the identifying ability at nighttime.

  - Effective date and Scope: As for the reverse triangle yellow portion of right and left sides and rear for vehicle of child-only vehicle and school bus, the vehicle types as of 2001/7/1, shall comply with this regulation.

  - Retro-reflective markings shall according to suitable types and range of principle: except for the brand and type series shall be the same, and also the same material, structure and installing ways.

  - Description of the function and specification: it shall describe material, structure and installing ways.

  - Inspection standard:

    - Color: shall be located within the following trichromatic coordinates

| Color | Yellow |
| --- | --- |
| Range of trichromatic coordinates |  | Ｘ | Ｙ |
|  | 1 | 0.545 | 0.454 |
|  | 2 | 0.487 | 0.423 |
|  | 3 | 0.427 | 0.483 |
|  | 4 | 0.465 | 0.534 |

    - Retro-reflection performance: shall comply with the following requirements.

| Observe angle | 0.33 degree (20') |
| --- | --- |
| Vertical incident angle | 0 degree |
| Horizontal incident angle | +5 degree -5 degree | +30 degree -30 degree | +40 degree -40 degree | +60 degree -60 degree |
| Minimum values for the yellow of Retro-reflection Unit: Cd/lx-m2 | 300 | 130 | 75 | 10 |

    - Weathering test:

Use Xenon arc lamp to light up, the illuminating time used is equivalent to the lighting time that makes the standard blue-7 cloth sample fade to gray-4. After the light-bake, the specimen shall comply with the following requirements:

      - No swelling, bubble, crack, peel-off, twist, spot or corrosion found on the specimen surface.

      - The color shall be within the range of trichromatic coordinates specified above.

      - At the condition of 0.33 degree-observation angle and +5 &-5 degree entrance angle, the minimum values for the yellow of retro-reflection shall be greater than 240 Cd＊lx-m2.